
[image: image1.png]



Broadcast Aggregate Exterior Florspartic 100 System Guideline Specification

DIVISION 09
FINISHES
PART  1  - GENERAL

1.1  
RELATED DOCUMENTS 

A.
Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 1 Specification Sections, apply to this section.

1. 2
SUMMARY

A.
Work specified in this section includes all labor, materials, equipment and services necessary to complete the proprietary Bomanite Broadcast Aggregate System including surface preparation, primers, aggregate and surface treatments.
B.
Related Sections include the following:

1. 
Division 1 Section “Product Requirements” for submittals and

substitutions.

2. 
Division 3 Section “Cast-in-Place Concrete” for concrete slabs. 

3.
Division 3 Section “Joint Sealers” Installation of caulking if required
1.3
SUBMITTALS
A. 
Product Requirements:

1. 
Provide submittal information within 35 calendar days after the contractor has received the owner's notice to proceed.

B. 
Product Data:

1. 
Submit Bomanite specifications, test data and other data required for each type of manufactured material and product indicated.

2. 
Submit Bomanite Technical Bulletins listing product name, descriptive data, curing time and application requirements.

3. 
Submit Bomanite Safety Data Sheet (SDS) and other safety requirements.

C.
Field quality-control test and inspection reports.

1.
Documentation by the Bomanite contractor of existing concrete condition and deficiencies prior to installation.
1.4
QUALITY ASSURANCE

A.
Installer Qualifications: The contractor for this work shall be a Bomanite Toppings System Licensee Licensed and Certified Applicator approved by Bomanite LLC
(303) 369-1115 or imagine@bomanite.com. 

1.
Provide letter of certification from Bomanite stating that installer is a certified applicator of special concrete finishes and is familiar with proper procedures/installation requirements of the manufacturer.

2.
Use an authorized Bomanite Licensee and adequate number of skilled workmen who are thoroughly trained and experienced in the necessary craft.

3.
Applicator shall be familiar with the specified requirements and the methods needed for proper performance of work of this section.

4.
Applicator shall be familiar with the previously approved samples and mock-ups that demonstrated standard of workmanship.

5.
Authorized Bomanite Toppings System installers limited to the following:
a.
www.bomanite.com/locate/  or approved by the Bomanite Company
b.
Marin Concrete Construction (951) 206-1640
B.
Manufacturer Qualifications: A firm experienced in the support and training of a national installer network and manufacturing products required/listed to complete the work.

1.
Bomanite LLC 303-369-1115 – no equal


C.
Source Limitations:
1.
Exterior Broadcast Aggregate System related materials: Obtain each type of material of the same brand from one source from a single manufacturer.

2.
Do not interchange manufactured materials within the Exterior Broadcast Aggregate System as all warranties whether expressed or implied will be null and void.
D.
Mock-ups:

1.
Apply finish to mock-ups constructed by Bomanite Licensed Installer, using each type of finish to demonstrate finished appearance and standard of workmanship.

a.
Mock-up shall include entire system, including surface preparation, primers, aggregate, expansion/isolation joints and surface treatments. 
b.
Notify Architect seven days in advance of dates and time when mock-ups will be constructed.

c.
Obtain from Architect approval of mock-ups before starting construction.

d.
If the Architect determines that the mock-ups do not meet requirements, General Contractor will demolish and remove them from the site and arrange to assemble more until approved.

e.
Maintain mock-ups during construction in an undisturbed condition as a standard for judging the completed work.

1.5
DELIVERY, STORAGE AND HANDLING

A. 
Deliver materials in original packages and containers, with seals unbroken, bearing Bomanite or Bomanite approved vendor labels indicating brand name and directions for storage, mixing with other components and application.

B. 
Store materials to comply with Bomanite written instructions to prevent deterioration from moisture or other detrimental effects.

C. 
Dispense special concrete finish material from Bomanite factory numbered and sealed containers. Maintain record of container numbers.

1.6
PROJECT CONDITIONS

A. 
Environmental Limitations:

1.
Comply with Bomanite written instructions for ambient temperature and other conditions affecting installation performance.

2. 
Concrete must be cured a minimum of 14 days or as directed by the manufacturer before installation of Bomanite Exterior Broadcast Aggregate System can begin.

1.7
PERFORMANCE REQUIREMENTS

A. The system is required to resist water intrusion indefinitely provided no structural movement has compromised the system.
B. The system is required to have a clear non-yellowing high-performance coating applied as a topcoat with a non-slip finish.
C. The system is required to have resistance to common solvents.
D. The system is required to suppress moisture and alkalinity for exterior use. 
PART  2  - PRODUCTS

2.1  
MANUFACTURERS 

A.
In other Part 2 articles where titles below introduce products, the following requirements apply to product selection:

1.
Available Manufacturers: Subject to compliance with requirements, manufacturers offering materials required to be incorporated into the work include, and are limited to, manufacturer listed. 


a. 
Bomanite (303) 369-1115 www.bomanite.com 
2.2
MATERIALS
A. 
Bomanite Florspartic 100 Gloss: A topically applied 100% solids hybrid Polyurea coating designed to be applied to correctly prepared wood, concrete and engineered cementitious products along with manufacturer approved epoxies. 
B.
XP Primer VB: 100% solids epoxy primer designed for exterior applications where moisture and alkalinity must be suppressed prior to the installation of a non-breathable high-performance coating or topping.

C. 
Broadcast Aggregate: Factory blended, UV stable sub-angular ceramic and quartz aggregates. 
D.
Bomanite Florthane SB95: 95% solids semi-gloss UV stable, chemically resistant urethane topcoat with aluminum oxide additives for improved abrasion and traction control. 

E.
No substitutions or alternates to the above will be accepted.

PART 3 – EXECUTION

3.1
EXAMINATION
A.
Consult General Contractor, Structural Engineer, Architect and Concrete Contractor with Bomanite installer present prior to pouring the concrete slab to which the Bomanite Exterior Broadcast Aggregate System is to be applied to. Ensure complete understanding of substrate preparation, vapor barrier installation, control joint placement, penetrations, mechanical bases, slope to drains etc. 
B.
Examine slab prior to installation with Bomanute installer present for conditions affecting performance of the Bomanite Exterior Broadcast Aggregate System. Rectify conditions detrimental to timely and proper work . Do not proceed with installation of Bomanite Exterior Broadcast Aggregate System until unsatisfactory conditions are corrected.
C.
Repair of defective portions of concrete slab due to improper installation is the responsisbility of the Bomanite installer. 
3.2
SURFACE PREPARATION
A.
Mechanically profile the concrete slab with walk behind grinders and hand held grinders to International Concrete Repair Institute Concrete Surface Profile 3 standards or greater. 
B.
Treat all cracks and control joints with a semi-rigid penetrating polyurea or equal two component product in a manner consistent with the repair product manufacturer’s guidlines. Grind the repair flush to the concrete slab prior to the Bomanite Exterior Broadcast Aggregate System installation.
C.
Construction and Contraction/Expansion/Isolation Joints:

1.
If necessary clean joints mechanically using hand held or walk behind grinders with crack chasing type blade after substantial completion of  the Bomanite Exterior  Broadcast Aggregate System.

2.
Fill all joints with  a flexible polyurethane joint filler in a manner consistent with the joint filler product manufacturer’s guidelines.
3.3
INSTALLATION
A.
Apply the Bomanite Exterior Broadcast Aggregate System according to the manufacturers proprietary internal application procedures including  prime coats, pigmented basecoats, aggregate, clear topcoat and joint fillers.
3.4
PROTECTION

A. It is the General Contractor’s responsibility to provide and install protection according to Bomanite installer’s recommendations. Protection of the finished surface is to be maintained by the General Contractor until substantial completion of the project is met and the floor can go into service. 

END OF SECTION
[image: image2.png]



International Society

OVER 1000 CONTRACTORS WORLDWIDE

The Bomanite International Society of licensed contractors is a worldwide network of specially trained and equipped professionals. Through constant exchange of new ideas, re-education and development programs, members of the Bomanite International Society continue to increase already high standards of quality and service. The activities of the Bomanite International Society are independent specialty contractors coordinated by Bomanite LLC. Bomanite also provides services and technical assistance to its member licensees, and to architects, designers and engineers specifying Bomanite products. For more information, including a list of members of the Bomanite International Society, contact:

Bomanite LLC – Technical Services
34501 E Quincy Ave
Building 28

Watkins, CO
Tel: (303) 369-1115 
imagine@bomanite.com
Web site: www.bomanite.com

© Copyright 2024 Bomanite Company.  Bomanite® is a registered trademark and servicemark with the U.S. Patent Office and other countries. 
