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Micro-Top ST Topping System Guideline Specification

DIVISION 09
FINISHES
PART  1  - GENERAL

1.1  
RELATED DOCUMENTS 

A.
Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 1 Specification Sections, apply to this section.

1. 2
SUMMARY

A.
Work specified in this section includes all labor, materials, equipment and services necessary to complete the Bomanite Micro-Top ST Topping System including surface preparation, primers, cementitious topping, and surface treatments.
B.
Related Sections include the following:

1. 
Division 1 Section “Product Requirements” for submittals and

substitutions.

2. 
Division 3 Section “Joint Sealers” Installation of caulking if required
1.3
SUBMITTALS
A. 
Product Requirements:

1. 
Provide submittal information within 15 calendar days after the contractor has received the owner's notice to proceed.

B. 
Product Data:

1. 
Submit Bomanite specifications, test data (if applicable) and other data required for each type of manufactured material and product indicated.

2. 
Submit Bomanite Technical Bulletins listing product name, descriptive data, curing time and application requirements.

3. 
Submit Bomanite Safety Data Sheet (SDS) and other safety requirements.

C.
Field quality-control test and inspection reports.

1.
Documentation by the Bomanite contractor of adequate surface profile prior to installation.
2.
Moisture tests of the concrete to be topped resulting in a reading of 85% or greater relative humidity are unacceptable for this type of installation. Consult with the Bomanite installer or Bomanite Technical Services on an appropriate system designed to suppress the moisture prior to installation.
1.4
QUALITY ASSURANCE

A.
Installer Qualifications: The contractor for this work shall be a Bomanite Toppings System Dealer and Certified Applicator approved by Bomanite Company
(303) 369-1115. 

1.
Provide letter of certification from Bomanite Company stating that installer is a certified applicator of special concrete finishes and is familiar with proper procedures/installation requirements of the manufacturer.

2.

Applicator shall be familiar with the specified requirements and the methods needed for proper performance of work of this section.

3.
Applicator shall be familiar with previously supplied project samples and have constructed mock-ups approved by the architect that demonstrate standard of workmanship.

4.
Authorized Bomanite Toppings System installers limited to the following:
a.  http://bomanite.com/find-licensed-contractors/
b. For additional assistance in locating an Authorized Bomanite Toppings Systems contact imagine@bomanite.com 
B.
Manufacturer Qualifications: A firm experienced in the support and training of a national installer network and manufacturing products required/listed to complete the work.

1.
Bomanite Company (303) 369-1115– no equal


C.
Source Limitations:
1.
Micro-Top ST related materials: Obtain each type of material of the same brand from one source from a single manufacturer.

2.
Do not interchange manufactured materials within the Micro-Top ST systems as all warranties whether expressed or implied will be null and void.
D.
Mock-ups:

1.
Apply finish to mock-ups constructed by Bomanite Certified Applicator, using each type of finish to demonstrate finished appearance and standard of workmanship.

a.
Mock-up shall include entire system, including surface preparation, primers, cementitious basecoat, cementitious topcoat, expansion/isolation joints and surface treatments. 
b.
Notify Architect seven days in advance of dates and time when mock-ups will be constructed.

c.
Obtain from Architect approval of mock-ups before starting construction.

d.
If the Architect determines that the mock-ups do not meet requirements, General Contractor will demolish and remove them from the site and arrange to assemble more until approved.

e.
Maintain mock-ups during construction in an undisturbed condition as a standard for judging the completed work.

1.5
DELIVERY, STORAGE AND HANDLING

A. 
Deliver materials in original packages and containers, with seals unbroken, bearing Bomanite or Bomanite approved labels indicating brand name and directions for storage, mixing with other components and application.

B. 
Store materials to comply with Bomanite written instructions to prevent deterioration from moisture or other detrimental effects.

C. 
Dispense special concrete finish material from Bomanite factory numbered and sealed containers. Maintain record of container numbers.

1.6
PROJECT CONDITIONS

A. 
Environmental Limitations:

1.
Comply with Bomanite written instructions for ambient temperature and other conditions affecting installation performance.

2. 
Concrete must be cured a minimum of 14 days or as directed by the manufacturer before installation of Bomanite Micro-Top ST can begin.

PART  2  - PRODUCTS

2.1  
MANUFACTURERS 

A.
In other Part 2 articles where titles below introduce products, the following requirements apply to product selection:

1.
Available Manufacturers: Subject to compliance with requirements, manufacturers offering materials required to be incorporated into the work include, and are limited to, manufacturer listed. 


a. 
Bomanite Company (303) 369-1115 www.bomanite.com
2.2
MATERIALS
A.
Bomanite Micro-Top ST: A cementitious topping comprised of powders in multiple gradations, field added vinyl versatate based polymer admixtures and other modifiers designed for a resilient coating. 

B. 
Bomanite Hydrolock: A semi-penetrating epoxy modified sealer with minimal residual surface sheen designed to protect cementitious surfaces.  
C.
No substitutions or alternates to the above will be accepted.

PART 3 – EXECUTION

3.1
EXAMINATION
A.
Consult the General Contractor, Structural Engineer, Architect and Pre-Cast Contractor with Bomanite installer present prior to casting the concrete to which the Micro-Top ST is to be applied to. Ensure complete understanding of substrate preparation, finishing, bond breakers or release agents, penetrations, expansion joints, moisture content etc. 
B.
Examine previously cast concrete prior to installation with Bomanute installer present for conditions affecting performance of the Micro-Top ST. Rectify conditions detrimental to timely and proper work . Do not proceed with installation of Micro-Top ST until unsatisfactory conditions are corrected.
3.2
SURFACE PREPARATION
A.
Mechanically profile the concrete slab with planetary head grinders, hand held grinders, shotblasting equipment, sandblasting (or other media deemed appropriate) or high pressure water cleaning equipment to ICRI CSP 1 or greater. 
3.3
INSTALLATION
A.
Apply the Micro-Top ST via four step spray application according to the manufacturers proprietary internal application procedures including field mixed primer, cementitious basecoat, cementitious topcoat and penetrating sealer.
B.
Application will have mockup present during installation to judge quality of workmanship and finished appearance. 
3.4
JOINTING

A.  
Expansion Joint Caulking: Joint caulking to be installed after the Micro-Top ST installation is complete.
B.  
All joints are to be diamond saw cut clean at transition or masked appropriately to have a relatively smooth and straight transition to caulking. 
C. 
Use a two component polyurethane or equal in a color complimentary to the Micro-Top ST System color. 
3.5
PROTECTION

A. General Contractor’s responsibility to provide and install protection according to Bomanite installer’s recommendations. Protection of the finished surface is to be maintained by the General Contractor until substantial completion of the project is met. 

END OF SECTION
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International Society

OVER 225 CONTRACTORS WORLDWIDE

The Bomanite International Society of licensed contractors is a worldwide network of specially trained and equipped professionals. Through constant exchange of new ideas, re-education and development programs, members of the Bomanite International Society continue to increase already high standards of quality and service. The activities of the Bomanite International Society are coordinated by The Bomanite Company. The Bomanite Company also provides services and technical assistance to its member Licensed Contractors, and to architects, designers and engineers specifying Bomanite products. For more information, including a list of members of the Bomanite International Society, contact:

Bomanite LLC
34501 East Quincy Ave. Building 28
Watkins, CO 80137
Tel: (303) 369-1115
Web site: www.bomanite.com
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