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Micro-Top with Bomanite Repair Mortar SH 
Guideline Specification
SECTION 03920
CONCRETE RESURFACING 

PART  1   GENERAL

1.1  
SECTION INCLUDES


A. 
This section includes the following:

1. Work of this section includes all labor, materials, equipment and services necessary to complete Bomanite Micro-Top system including cementitious fill, clear coatings and maintenance finishes.
1.2  
RELATED SECTIONS

A. 
Related Work:

1. Section 09820 Polymerized Cementitious Flooring

2. Section 09620 Specialty Flooring

3. Section 03300 Concrete
1.3  
SUBMITTALS

A. 
Comply with pertinent provisions of Section 01600 – Product Requirements.

1. 
Provide submittal information within 35 calendar days after the contractor has received the owner's notice to proceed.

B. 

Product data:

1. 
Submit special concrete finishes manufacturer’s specifications, test data and other data required for each type of manufactured material

    

and product indicated.

2. 
Submit special concrete finishes technical bulletins giving manufacturer’s name, product name, and product line number for the 

     

specified material proposed to be provided under this section.

3. 
Submit special concrete finishes technical data sheet giving descriptive data, curing time, and application requirements.

4. 
Submit special concrete finishes manufacturer’s Material Safety Data Sheet (MSDS) and other safety requirements.

1.4  
DELIVERY, STORAGE, AND HANDLING

A.  
Store products in manufacturer's unopened packaging until ready for installation.

B.  
Store and dispose of solvent-based materials, and materials used with solvent-based materials, in accordance with requirements of local authorities having jurisdiction.

1.5  
QUALITY ASSURANCE

A. The contractor for this work shall be a licensed Bomanite Toppings Systems Licensee Certified Applicator trained and equipped by:
The Bomanite Corporation (303) 369-1115 – no equal

B. 
Installer Qualifications:

1. Use an authorized Bomanite Toppings Systems Licensee and adequate number of skilled workmen who are thoroughly trained and  experienced in the necessary craft         
2. Applicator shall be familiar with the specified requirements and the methods needed for proper performance of work of this section.

C. 
Manufacturer’s Certification:

1. Provide letter of certification from The Bomanite Company stating that installer is a certified applicator of special concrete finishes and is familiar with proper procedures/installation requirements required by the manufacturer.

D. 
Mock-ups:

1. Apply mock-ups of each type finish, to demonstrate typical joints, surface finish, color variation (if any), and standard of workmanship.

a. Build mock-ups approximately 100 square feet in the location indicated or if not indicated, as directed by the Architect or Owner Representative.

b. Notify Architect or Owner Representative seven days in advance of dates and times when mock-ups will be constructed.

c. Obtain from the Architect or Owner Representative approval of mock-ups before starting construction.

d. If the Architect or Owner Representative determines that mock-ups do not meet requirements, demolish and remove them from the site and cast others until mock-ups are approved.

e. Maintain mock-ups during construction in an undisturbed condition as a standard for judging the completed work.

1.6  
DELIVERY, STORAGE, AND HANDLING

A. 
Deliver materials in original packages and containers, with seals unbroken, bearing manufacturer labels indicating brand name and  

     

directions for storage, mixing with other components, and application.

B. 
Store materials to comply with manufacturer’s written instructions to prevent deterioration from moisture or other detrimental effects.

C. 
Dispense special concrete finish material from factory numbered and sealed containers. Maintain record of container numbers.

1.7  
PROJECT CONDITIONS

A. 
Environmental limitations:

1.
Comply with manufacturer’s written instructions for substrate temperature and moisture content, ambient temperature and 

humidity, ventilation, and other conditions affecting installation performance.

2. 
Concrete must be cured a minimum of 28 days or as directed by the manufacturer before application of Bomanite Self Leveler can begin.

B. 
Close areas to traffic during and after floor application for time period recommended in writing by licensed installer.

PART  2   PRODUCTS

2.1  
MANUFACTURERS MATERIALS


A. 
Polymerized Cementitious Flooring
1. Bomanite XP Primer

2. Bomanite Repair Mortar SH
3. Bomanite Micro-Top and related tint packs, polymer, etc.
4. No substitutes will be considered or allowed.
B. 
Hardening/sealing agent

1. Bomanite HydroLock
2. Bomanite Floor Finish
3. No substitutes will be considered or allowed.

2.2  
APPLICATIONS/SYSTEM

A. 
Decorative trowel-applied Micro-topping:  Bomanite Micro-Top; Pre-blended, field tinted, cementitious, abrasion-resistant, suitable as exposed wear layer over concrete; maximum thickness 1/8 inch.
1. 
Primer:  Bomanite XP Primer
2.
Color: Bomanite Tint Packs

B. 
Interior trowel-applied underlayment:  Bomanite Repair Mortar SH: Pre-blended, cementitious, abrasion-resistant, suitable as a fill material over concrete; minimumthickness ¼ inch, maximum thickness 2 inch.
1. 
Primer:  Bomanite XP Primer
PART  3   EXECUTION

3.1  
EXAMINATION


       A.

Examine the areas and conditions where polymerized cementitious flooring system is to be installed and notify the Architect and General Contractor of conditions detrimental to the proper and timely completion of the work. Do not proceed with the work until unsatisfactory conditions have been corrected by the General Contractor in a manner acceptable to both the Architect and the Installer. 

B. 
Verify that concrete slab meets a minimum of 3500 psi of compressive strength. Consult American Concrete Institute ACI302.IR-89, Guide for Concrete Floor and Slab Construction requirements in Division 3 Section "Cast-In-Place Concrete," and Project Conditions.   
3.2  
PREPARATION

A. 
Apply Micro-Top by Bomanite over Bomanite Repair Mortar SH cementitious fill, direct bonded to concrete substrate in accordance with manufacturer’s proprietary, internal application procedures. 

3.3  
INSTALLATION

A. 
Install in accordance with manufacturer's instructions.

1. Mechanical abrasion of concrete slab to create profile necessary to allow correct bonding system
4. Installation into tacky XP Primer, mixed Bomanite Repair Mortar SH at a nominal thickness of 3/4 inch 

5. After adequate cure time, installation of Bomanite Micro-Top Basecoats and Finish coats in such a manner as to satisfy mockups and Architects pre-determined colors and textures.



6. After adequate dry time, installation of protection by General Contractor
3.4  
PROTECTION

A. Protect finished work until fully cured in accordance with manufacturer’s recommendations.

END OF SECTION
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International Society

OVER 225 CONTRACTORS WORLDWIDE

The Bomanite International Society of licensed contractors is a network of specially trained and equipped professionals. Through constant exchange of new ideas, re-education and development programs, members of the Bomanite International Society continue to increase already high standards of quality and service. The activities of the Bomanite International Society are coordinated by The Bomanite Company. The Bomanite Company also provides services and technical assistance to its member licensees, and to architects, designers and engineers specifying Bomanite products. For more information, including a list of members of the Bomanite International Society, contact:

Bomanite LLC
34501 East Quincy Ave. Building 28
Watkins, CO 80137
Tel: (303) 369-1115
Website: www.bomanite.com 
© Copyright 2026 Bomanite LLC. Bomanite® and Micro-Top® are registered trademark and service mark with the U.S. Patent Office and other countries.


